## Slide 1
T22 PA8536 ESD
Verify Result & Analysis
July, 2019

## Slide 2: T22 IO/ESD Testing
HBM/MM Test Result list in Table 1
  VH_1: 1.8V
  VH_2 (A): 0.9V
    PLLS_AVDD09/PLLS_DVDD09
  VH_2 (A): 0.9V
    TX_VDD09
  IO : GPIO (5VT cell)
Root Cause Summary
  VH_2 (B): Described later in next page
  5VT summary as following
PASS | HBM | MM
VH_1-VG | 3KV | 250V
VH_2-VG (A) | 3KV | 300V
VH_2-VG (B) | 2KV | 150V
IO-VG | 3KV | 150V
Table 1 ESD Test Result Summary
Fig. RST_N hot spot and PFA locage NMOS drain side damage at MM200V

## Slide 3: MM Solution by Himax
Modify the entry site of RST_N cell  VIA5
(avoid the current limit at entry site)
High voltage-tolerant Solution
Create auxiliary pad to enhance ESD level (not recommended)
  Need to check functionality for integrated pad
High Voltage Tolerant
Circuit Illustration
Auxiliary pad

## Slide 4: MM Failure Analysis TX_VDD09 (pin 27) Result
Pattern+ emission(20X)
MM +200V failure location
  Measurement condition
  Layout check on going
  PFA on going

## Slide 5: IP0956 TX_VDD09 MM=200V Damage Location
VSSA18
內部點, 無出PAD
VSSA18
MM fail: TX_VDD09 – GND group
Dummy region

## Slide 6: Damage Circuit Evaluation  Perc condition reference
ESD
GND
Damage
Turn-on
W/L=
1000u/0.15u,
MPG
通常這點為內部電路, P & NMOS 2 junction 不會ESD fail.
發生條件為: MPG size夠大, gate node floating.
當ESD來時, MPG 有機會turn on, 以至core is weak because of ESD rule 而被damage.
TX_VDD09

## Slide 7: IP0956 TX_VDD09 MM=200V Damage Location
VSSA18
Dummy region (藍色虛線框)
TXVDD09  VSSA18 direct clamp
Ideal path
Damage path into core
2. Cap inserted in between core to VSSA
TX_VDD09
VSSA18
Direct
Clamp